## Slide 1
Durable Antireflective, Anti-Soiling, and Self-Cleaning Glass for Solar Modules
Reflection at the air/glass interface due to an instantaneous change in the index of refraction
Demonstrated broad angle (0.4% at 0° incidence) and broadband antireflection (4.9% at 65°)
Irregular like nanostructures on the glasswing butterfly
Superomniphobic glass repellent to a wide array of liquids and particles
Particulates adhere weakly to surface and are easily removed by dew condensation
Improve scalability of processing to > 20 cm x 20 cm areas
Demonstrated less than 5% decrease in transmission with soiling
Demonstrate silicon minimodule environmental durability
Corning
Dr. Carl E. Crossland
Pitt
Dr. Paul W. Leu
Sajad Haghanifar
Sooraj Sharma
Benjamin Bailey
NETL
Dr. Paul Ohodnicki
Dr. Bryan D. Morreale
Soiling from particulates/pollutants lead to as much as ~60% efficiency loss!
Efficiency Loss Issues
Ready! Goals Met
Anti-Soiling and Self-Cleaning
Antireflection
Proposed Work
Key Personnel/Organizations
Milk
Blood
Water
Coffee
Ethylene Glycol
Cranberry Juice
Orange Juice
Performance Metrics | Units | Goals | Actual
Scalable Fabrication | Area | > 10 cm x 10 cm | 10 cm x 10 cm
Broadband Antireflection | % Reflection (wavelengths 400 to 1100 nm) | < 1 | 0.4%
Broad Angle Antireflection | % Reflection at 45° | < 2 | 4.9% at 65°
Static Water Contact Angle | Degrees | > 155 | 162.1  2.0°
Water Contact Angle Hysteresis | Degrees | < 5 | 3.2  0.7°
Self-Cleaning Tests | % Decrease in Transmission | < 5 | < 1
Cost | $/m2 | < 20 |  20
Mechanical Durability (ASTM D1044 Abrasion Tests) | % Change in Optical and Wetting Properties | < 10 | < 5